| OWNER/AGENT | Elizabeth Otto |
| --- | --- |
| OWNER’S ID NR. | N/A |
| DATE RECEIVED | November 8th, 2024 |
| EXAMINER | Margaret Priest |
| FACULTY SUPERVISOR(S) | Emily Hamilton |
| DATE OF REPORT | September 18th, 2025 |
| # ARTIST/MAKER (Owner Attribution) | Margarete (Grete) Heymann-Loebenstein (later Marks) |
| SIGNATURE and its LOCATION | N/A |
| TITLE (“”) or DESCRIPTION | Egg cup from ceramic breakfast set |
| DATE | c. 1923 – 1934 |
| STRUCTURE | Stoneware |
| DIMENSIONS (H x W x D) | 2 ¼” x 2 1/16” diameter (5.7 cm x 5.2 cm diameter) |
| ACCESSORIES | N/A |
| LABELS/DISTINGUISHING MARKS | 289/31 and maker’s mark in dark blue |

### OBSERVATIONS DURING TREATMENT

XRF analysis of the glaze confirmed the presence of heavy metals, specifically lead, tin, and uranium, in the glaze and clay body. Other elemental findings are enumerated in Analysis and Imaging document.

### TREATMENT PERFORMED

- Written and photographic documentation was completed prior to, during, and following treatment to record condition and procedures.

- The surface was gently dry cleaned with a cosmetic sponge to remove dust.

- Solubility testing with acetone and ethanol was performed to determine if the target adhesive would be suitable for the glaze. Both colors of glaze were found to be insoluble in both solvents.

- The fragments were reassembled with a 40% solution of Paraloid B-72 dissolved in a 1:1 solution of acetone and ethanol.

- Small cracks left in the surface were filled with Flügger to match the surface texture of the cup.

- The Flügger fills were inpainted with acrylic paints to match the glaze.

- Inpainted fills were sealed with a 1:1 blend of glossy and matte acrylic media.

Swisspers Premiun Cosmetic Wedges, polyurethane foam.

A copolymer of ethyl methacrylate methylacrylate; Conservator’s Emporium; 100 Standing Rock Cir., Reno, NV 89511;  (775) 852-0404 · FAX (775) 852-3737.

Acetone, Fisher Scientific Company, Pittsburgh, PA 15219.

Ethanol, Fisher Scientific Company, Pittsburgh, PA 15219.

Flugger Acrylic Spackle, Flügger  Islevdalvej 151  DK-2610 Rødovre Denmark.

Golden Fluid Acrylics, (100% acrylic emulsion artist paints), Golden Artist Colors, Inc., 188 Bell Rd, New Berlin, NY 13411.

Golden Polymer Varnish with UVLS (Gloss), Acrylic solution polymer varnish with ultraviolet filters and light stabilizers, Golden Artist Colors, Inc., 188 Bell Rd, New Berlin, NY 13411.

Golden Polymer Varnish with UVLS (Matte), Acrylic solution polymer varnish with ultraviolet filters and light stabilizers, Golden Artist Colors, Inc., 188 Bell Rd, New Berlin, NY 13411.